To:                                                                                Specification No.:

# Delivery Specification

Product Name: TPU Paint Protection Film

Model No.:

Date of Establishment:

| Manufacturer | Buyer |
| --- | --- |
| 泰浪商务 |  |

## 1. Scope of Application

This specification applies to the TPU paint protection film  produced by 泰浪商务

product name：

model No.:

Buyer：

## 2. Purpose

This specification is formulated to ensure the delivery quality of the TPU paint protection film

Product name：

Model No.:

## 3. Product Form

### (1) Structure

The product adopts a 5-layer structure:

2.0mil Toray high-definition protective film on the surface,

0.28mil Kaxiu repair coating,

particle TPU substrate (        mil),

1.2mil Bostik Aroset pressure-sensitive adhesive layer, and 3mil release film.

|  | 2.0mil Toray high-definition protective film |
| --- | --- |
|  | 0.28mil Japanese-style repair coating |
|  | Aliphatic polycaprolactone TPU substrate |
|  | 1.2mil Bostik Ashland pressure-sensitive adhesive layer |
|  | 3mil matte release film |

### (2) Shape

The product is in film form, cut to a length of 15m and a width of 1524mm, wound into a roll on a 3-inch (1 inch = 25.4mm) plastic tube with the release film layer as the inner surface.

### (3) Splicing

No splicing.

## 4. Packaging and Marking

### (1) Packaging Form

① A 3-inch plastic tube is used as the core, and the product is packaged in a suspended manner.
② The inner packaging is fully wrapped with polyethylene film.
③ The outer packaging is bundled with corrugated paper.

### (2) Label

① Product labels are affixed to the inner side of the product roll core and the side of the outer corrugated carton.
② The product label contains the following information:
Model No.:
Size: 1.524m*15m
Traceability No.: Refer to the description in "(3)" below

### (3) Definition and Explanation of Batch Number

① One batch is defined as one continuous production of the same product type.
② The batch number consists of the following numbers and English letters.
(Example) S1A1001CF1001

Finished Product Serial Numbers

S1A1001    CF1           001
Production Order No：

Rewinding Team

## 5. Product Quality Specifications

The TPU paint protection film (product name, model No.: ) meets the following specifications for each item:

| Test Item |  | Test Method | Unit | Specification Standard Value |
| --- | --- | --- | --- | --- |
| Thickness | Total Thickness | GB/T 6672 | μm |  |
|  | Usable Layer Thickness |  | μm |  |
| Width |  | GB/T 6673 | mm | 1522±2 |
| Product Elongation at Break |  | ASTM D-882 | % | ≥300 |
| Tensile Strength |  | ASTM D-882 | MPa | ≥16 |
| Elastic Modulus |  | ASTM D-882 | Kgf/cm² | 180≤E≤350 |
| UV Barrier Rate |  | GB/T 2680 | % | ≥90 |
| Haze |  | ASTM D1003 | ≤ | 2.0 |
| Adhesive Force | Initial Adhesion | Test 20 minutes after pasting on steel plate | N/in | 15≤F≤25 |
|  | Permanent Adhesion | Test 168 hours after pasting on steel plate |  | 20≤F≤30 |
| Elongation at Break of Repair Layer |  | ASTM D-882 | % | ≥180 |
| Acid and Alkali Resistance |  | Immerse in HCl solution (pH 2~3) and NaOH solution (pH 13~14) for 30 minutes respectively | / | No abnormality |
| Special Requirement Test Method |  | Film pasting test is normal |  |  |

## 6. Submitted Materials

Factory quality inspection report: Test shall be carried out according to the manufacturing batch, and the factory quality inspection report shall be provided in the format of Annex I.

## 7. Validity Period

This delivery specification is valid for 1 year from the date of establishment. After the expiration of the period, both parties shall confirm whether modification or update is required.

# Annex I: 泰浪商务 Paint Protection Film Finished Product Inspection Report

| Product Code |  |  |  |  | Production LOT |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- |
| Production Order No |  |  |  |  | Manufacturing Date |  |  |
| Test Item |  |  | Test Method | Unit | Standard Value | Test Result | Judge |
| Appearance |  |  | Visual inspection | / | Meet product appearance quality requirements |  |  |
| Thickness | Total Thickness |  | GB/T 6672 | μm | 328±10 |  |  |
|  | Usable Layer Thickness |  |  | μm | 186±10 |  |  |
| Width |  |  | GB/T 6673 | mm | 1522±2 |  |  |
| Product Elongation at Break |  |  | ASTM D-882 | % | ≥300 |  |  |
| Tensile Strength |  |  | GB/T 17657-2013 | MPa | ≥16 |  |  |
| Elastic Modulus |  |  | ASTM D-882 | Kgf/cm² | 180≤E≤350 |  |  |
| UV Barrier Rate |  |  | GB/T 2680 | % | ≥90 |  |  |
| Haze |  |  | ASTM D1003 | % | ≤2.0 |  |  |
| Adhesive Force |  | Initial Adhesion | Test 20 minutes after pasting on steel plate | N/in | 15≤F≤25 |  |  |
|  |  | Permanent Adhesion | Test 168 hours after pasting on steel plate |  | 20≤F≤30 |  |  |
| Elongation at Break of Repair Layer |  |  | ASTM D-882 | % | ≥100 |  |  |
| Repairability |  |  | Scratch 30 times with fine copper brush under 200g/cm² load, repair with 70℃ hot water or hot air | S | ≤5 |  |  |
| Scratch Resistance |  |  |  | / | No scratch |  |  |
| Acid and Alkali Resistance |  |  | Immerse in HCl solution (pH 2~3) and NaOH solution (pH 13~14) for 30 minutes respectively | / | No abnormality |  |  |
| Special Requirement Test Method |  |  |  |  |  |  |  |
| Comprehensive Judgment |  |  |  |  | Inspection Date |  |  |
| Inspector |  |  |  |  | Reviewer |  |  |
| Remarks |  |  |  |  | </ |  |  |